### THERMOPADS PVT. LTD.

### HYDERABAD

| TECHNICAL DATA | Section No. : TPL/TD/28 Issue/Rev. No. : 08/02 Date : 15.05.2014 Page No. : 1 |
| --- | --- |
| Temperature and Speed maintained on ROSENDAHL Extruder (TPL/M/60) |  |

| For ECTFE Compound (HALAR) Temp in Deg C. Tolerance +/- 30 deg C |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Z1 | Z2 | Z3 | Z4 | Flange | H1 | H2 | Die | Water (+/-10 deg C) | Gap between Head to Hot water zone | Pre Heater ( % heat set) | Resistance Pre Heater | Output Kg/hr |
| 200 | 240 | 250 | 250 | 250 | 260 | 265 | 265 | 40 | 1 – 2 Feet | 20-60 | Nicr 10 –15 A Adv 10 – 15 A Mid 10 – 15 A |  |

Preheating temp : 250+/-20degC for resistance alloy wire& for NPC 200+/-20degC+/-20

| For ETFE (Tefzol) & FEP Compound Temp in Deg C. Tolerance +/- 20 deg C |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Z1 | Z2 | Z3 | Z4 | Flange | H1 | H2 | Die | Water (+/-10 deg C) | Gap between Head to Hot water zone | Pre Heater ( % heat set) | Resistance Pre Heater |
| 280 | 290 | 310 | 330 | 340 | 350 | 360 | 370 | 40 | 0.5-1.5 Mtr | 20 – 60 | Nicr 10 –15 A Adv 10 – 15 A Mid 10 – 15 A |

### Setting of heater with preheater model No……….

MFS, Recommended DDR & DBR…

Any other parameter required….

### THERMOPADS PVT. LTD.

### HYDERABAD

| TECHNICAL DATA | Section No. : TPL/TD/28 Issue/Rev. No. : 08/03 Date : 15.05.2014 Page No. : 2 |
| --- | --- |
| Temperature and Speed maintained on ROSENDAHL Extruder (TPL/M/60) |  |

| For PFA Compound Temp in Deg C. Tolerance +/- 20 deg C |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Z1 | Z2 | Z3 | Z4 | Flange | Neck | Head | Die | Water (+/-10 deg C)4 | Gap between Head to Hot water zone | Pre Heater ( % heat set) | Heat Selection |
| 320 | 350 | 365 | 370 | 370 | 380 | 385 | 390 | 50 | 1.5 to 2.0 m | 80 to 100 | 2 |

| For PA11 Compound Temp in Deg C. Tolerance +/- 20 deg C |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Z1 | Z2 | Z3 | Z4 | Flange | H1 | H2 | Die | Water | Gap between Head to Hot water zone | Pre Heater ( % heat set) | Resistance Pre Heater |
| 160 | 170 | 175 | 180 | 180 | 190 | 195 | 200 | ------ | 1-2 Feet | ------- | ------- |

Note:

- Temperature will vary depending on Line speed and ambient temperature.

- Whenever online Corona is required, Corona voltage will be maintained 0.3 - 0.4KV

- The curing shall be air curing for PFA insulation with the insulation thickness < 0.40 mm.

- For PFA insulation with the insulation thickness > 0.40mm

THERMOPADS PVT. LTD

HYDERABAD

| TECHNICAL DATA | Section No. : TPL/TD/28 Issue/Rev. No. : 08/02 Date : 15.05.2014 Page No. : 03 |
| --- | --- |
| Temperature maintained on MTT Extruder (TPL/M/91) |  |

| For ECTFE Compound Temp in Deg C. Tolerance ± 20° C |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ex1 | Ex2 | Ex3 | Ex4 | Clamp | H1 | Cartridge | Die nut | Water (+/-10 deg C) | Gap between Head to Hot water zone | Pre Heater ( % heat set) |
| 250 | 255 | 260 | 260 | 265 | 260 | 265 | 300 | 40 | 1- 2 Feet | 20-60 |

| For FEP & PFA Compound Temp in Deg C. Tolerance ± 20° C |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ex1 | Ex2 | Ex3 | Ex4 | Clamp | H1 | Cartridge | Die nut | Water (+/-10 deg C) | Gap between Head to Hot water zone | Pre Heater ( % heat set) |
| 280 | 285 | 300 | 310 | 320 | 335 | 350 | 370 | 50 | 1- 2 Feet | ---- |

| For ETFE (Tefzol) Compound Temp in Deg C. Tolerance +/- 20 deg C |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ex1 | Ex2 | Ex3 | Ex4 | Clamp | H1 | Cartridge | Die nut | Water (+/-10 deg C) | Gap between Head to Hot water zone | Pre Heater ( % heat set) | Resistance Pre Heater |
| 280 | 290 | 310 | 330 | 340 | 350 | 360 | 370 | 40 | 0.5-1.5 Mtr | ---- | ---- |

Note:  Temperature will vary depending on Line speed and ambient temperature.

### THERMOPADS PVT. LTD.

### HYDERABAD

| TECHNICAL DATA | Section No. : TPL/TD/28 Issue/Rev. No. : 08/01 Date : 15.05.2014 Page No. : 4 |
| --- | --- |
| Temperature and Speed maintained on WINDSOR Extruder (TPL/M/43) |  |

| For PVC Compound Temp in Deg C. Tolerance +/- 20 deg C |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Z1 | Z2 | Z3 | Z4 | Z5 | Z6 | H | D | Compound pre-heating temperature |
| 130 | 135 | 140 | 145 | 150 | 150 | 148 | 160 | 70 to 80 |

| For LSZH Compound Temp in Deg C. Tolerance +/- 20 deg C |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Z1 | Z2 | Z3 | Z4 | Z5 | Z6 | H | D | Compound pre-heating temperature |
| 120 | 125 | 135 | 140 | 145 | 150 | 145 | 155 | 75 to 85 |

Note:  Temperature will vary depending on Line speed and ambient temperature.

THERMOPADS PVT. LTD.

HYDERABAD

| TECHNICAL DATA | Section No. : TPL/TD/28 Issue/Rev. No. : 08/01 Date : 15.05.2014 Page No. : 5 |
| --- | --- |
| Temperature and Speed maintained on SUPERMAC Extruder (TPL/M/90) |  |

| For PVC & TPE Compound Temp in Deg C. Tolerance +/- 20 deg C |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Z1 | Z2 | Z3 | Z4 | Clamp | Neck | Head | Die | Compound pre-heating temperature PVC &TPE |
| 165 | 180 | 190 | 200 | 190 | 190 | 195 | 200 | 85°C to 95°C |

| For ZH & XL-ZH Temp in Deg C. Tolerance +/- 20 deg C |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Z1 | Z2 | Z3 | Z4 | Clamp | Neck | Head | Die | Compound pre-heating temperature for ZH | Compound pre-heating temperature for XL ZH |
| 140 | 145 | 150 | 155 | 150 | 150 | 150 | 155 | 75 to 85 | --------- |

Note:  Temperature will vary depending on Line speed and ambient temperature.

### THERMOPADS PVT. LTD.

### HYDERABAD

| TECHNICAL DATA | Section No. : TPL/TD/28 Issue/Rev. No. : 08/01 Date : 15.05.2014 Page No. : 6 |
| --- | --- |
| Temperature and Speed maintained on ROSENDAHL Extruder (TPL/M/125) |  |

| For ECTFE Compound Temp in Deg C. Tolerance ± 30° C |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Z1 | Z2 | Z3 | Z4 | Flange | H1 | H2 | H3 | H4 | Water (+/-10 deg C) | Gap between Head to Hot water zone | Pre Heater ( % heat set) | Resistance Pre Heater |
| 250 | 255 | 265 | 270 | 270 | 270 | 270 | 265 | 250 | 40 | 1-2 Feet | 20-100 | Nicr 10 –15 A Adv 10 – 15 A Mid 10 – 15 A |

| For ETFE Compound |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Z1 | Z2 | Z3 | Z4 | Flange | H1 | H2 | H3 | H4 | Water (+/-10 deg C) | Gap between Head to Hot water zone | Pre Heater ( % heat set) | Resistance Pre Heater |
| 280 | 290 | 310 | 330 | 340 | 350 | 360 | 365 | 370 | 40 | 1-2 Feet | 20-100 | Nicr 10 –15 A Adv 10 – 15 A Mid 10 – 15 A |

| For FEP & PFA Compound |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Z1 | Z2 | Z3 | Z4 | Flange | H1 | H2 | H3 | H4 | Water (+/-10 deg C) | Gap between Head to Hot water zone | Pre Heater ( % heat set) | Resistance Pre Heater |
| 320 | 350 | 365 | 370 | 370 | 380 | 385 | 385 | 390 | 50 | 1-2 Mtr | 20 – 100 | Nicr 10 –15 A Adv 10 – 15 A Mid 10 – 15 A |

| For PA11 Compound |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Z1 | Z2 | Z3 | Z4 | Flange | H1 | H2 | H3 | H4 | Water (+/-10 deg C) | Gap between Head to Hot water zone | Pre Heater ( % heat set) | Resistance Pre Heater |
| 160 | 170 | 175 | 180 | 180 | 190 | 190 | 195 | 200 | 50 | 1-2 Mtr | 20 – 100 | Nicr 10 –15 A Adv 10 – 15 A Mid 10 – 15 A |

THERMOPADS PVT. LTD.

HYDERABAD

| TECHNICAL DATA | Section No. : TPL/TD/28 Issue/Rev. No. : 09/00 Date : 26.06.2018 Page No. : 7 |
| --- | --- |
| Temperature and Speed maintained on SUPERMAC Extruder (TPL/M/132) |  |

| For PVC & TPE Compound Temp in Deg C. Tolerance +/- 20 deg C |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Z1 | Z2 | Z3 | Z4 | Clamp | Neck | Head | Die | Compound pre-heating temperature PVC &TPE |
| 165 | 180 | 190 | 200 | 190 | 190 | 195 | 200 | 85°C to 95°C |

| For ZH & XL-ZH Temp in Deg C. Tolerance +/- 20 deg C |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Z1 | Z2 | Z3 | Z4 | Clamp | Neck | Head | Die | Compound pre-heating temperature for ZH | Compound pre-heating temperature for XL ZH |
| 140 | 145 | 150 | 155 | 150 | 150 | 150 | 155 | 75 to 85 | --------- |

Note:

- Temperature will vary depending on Line speed and ambient temperature.

- For FPC–SR and GDIT-SR Outer jacket use chiller Temperature is 10 deg C & chiller length should be 6Mtrs.

### THERMOPADS PVT. LTD.

### HYDERABAD

| TECHNICAL DATA | Section No. : TPL/TD/28 Issue/Rev. No. : 08/00 Date : 27.06.2014 Page No. : 8 |
| --- | --- |
| Temperature and Speed maintained on SUPERMAC Extruder |  |

| For XLPE Compound Temp in Deg C. Tolerance ± 20° C |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Z1 | Z2 | Z3 | Z4 | Clamp | Neck | Head | Die |
| 150 | 165 | 170 | 175 | 170 | 180 | 210 | 250 |

Note :

- Catalyst to be preheated at 60deg C for 8-10hrs.

- The drafted polymer and catalyst to be manually mixed at ratio of 95 by 5 %

- Recommended start-up procedure is given below:

- Ensure that the screw, barrel and tools are thoroughly cleaned.

- Start up slightly lower temperature profile. Allow the frictional heat to build-up to desired temperature and remain steady thereafter.

- Flush with virgin LDPE (film grade). Adjust eccentricity and wall thickness inserting conductor.

- Replace LDPE with premixed drafted polymer and catalyst. Increase line speed to optimum. Adjust temperature to obtain a smooth surface finish.

- Avoid thermal shock by sudden cooling. Keep sufficient distance between die-head and water trough to allow air cooling. Avoid inlet water being too cold.

- It is important that extruder should not be kept idle for more that 15 minutes when filled premix compound.

THERMOPADS PVT. LTD.

HYDERABAD

| TECHNICAL DATA | Section No. : TPL/TD/28 Issue/Rev. No. : 08/00 Date : 15.05.2014 Page No. : 9 |
| --- | --- |
| Temperature and Speed maintained on SUPERMAC Extruder (TPL/M/90)or(TPL/M/132) |  |

| For LFH Material Temp in Deg C. Tolerance +/- 20 deg C |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Z1 | Z2 | Z3 | Z4 | Clamp | Neck | Head | Die | Compound pre-heating temperature for LFH |
| 140 | 145 | 150 | 155 | 150 | 150 | 150 | 155 | 75 to 85 |

Note:  Temperature will vary depending on Line speed and ambient temperature.

### THERMOPADS PVT. LTD.

### HYDERABAD

| TECHNICAL DATA | Section No. : TPL/TD/28 Issue/Rev. No. : 08/00 Date : 21.05.2018 Page No. : 10 |
| --- | --- |
| Temperature and Speed maintained on ROSENDAHL Extruder (TPL/M/125) |  |

| For FEP COMPOUND(CJ95 & NP20) For M/s. SIEMENS Temp Tol : +/-20° C |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Z1 | Z2 | Z3 | Z4 | Z5/Flange/ Clamp | Z6/H1 | H2/ Cartridge | Die | Water (+/-10° C) | Gap between Head to Hot water zone | conductor Temp (+/-10° C) | Load (Amp) | Line speed (m/min) (+/-3) | Screw Speed (RPM) (+/-2) |
| 324 | 348 | 355 | 365 | 380 | 375 | 380 | 390 | No water | Not applicable | 110°C | 18 | 22 | 30 |

Tool  Requirement :

Note:  Check visually conductor should not become Black/ Blackish